Heterogeneous flooring：

帮我把下面的参数翻译成英文

1、品牌：法福莱

2、材质：多层复合工艺，致密底

3、厚度：2.0mm，宽度：2米

3、耐污：表面UV耐污处理，易清洁打理

4、阻燃性：燃烧性能达到B1（C-S1，t0）级难燃材料

5、耐磨性：通过GB/T11982.1-2015检测依据，耐磨性能T级，椅子脚轮试验无破损

6、稳定性：内含玻璃纤维稳定层，加热尺寸变化率纵向0.08%，加热尺寸变化率横向0.05%。

7、甲醛释放量（GB/T 17657-2013）：符合EO等级要求

8、可溶性重金属（铅、镉）：＜0.1 mg/㎡

9、防滑性：通过DIN 51130-2014检测依据，达到R10级 15.4°

10、耐酸耐碱：通过ISO 26987:2008检测，氢氧化钠溶液（25%），盐酸溶液（3%），无影响

11、通过ISO9001、ISO14001、ISO45001认证

12、通过欧盟CE认证

13、《2024年中国弹性地板行业十大品牌》《2023年中国弹性地板行业十大品牌》《2022年中国弹性地板行业十大品牌》《2021年中国弹性地板行业十大品牌》《2018年中国弹性地板行业十大知名品牌》《2017年中国运动地板行业领军品牌》《2016年中国弹性地板行业十大流通品牌》

Brand: FARFLY

Material: Multi-layer composite technology, dense base

Thickness: 2.0mm, Width: 2 meters

Stain Resistance: Surface UV stain-resistant treatment, easy to clean and maintain

Flame Retardancy: Burning performance meets Class B1 (C-S1, t0) standard for flame-retardant materials

Wear Resistance: Tested according to GB/T 11982.1-2015, wear resistance grade T, no damage in chair caster test

Stability: Contains glass fiber stabilization layer, longitudinal heating dimensional change rate 0.08%, transverse heating dimensional change rate 0.05%

Formaldehyde Emission (GB/T 17657-2013): Complies with E0 grade requirements

Soluble Heavy Metals (Lead, Cadmium): <0.1 mg/m²

Slip Resistance: Tested according to DIN 51130-2014, achieves R10 grade 15.4°

Acid and Alkali Resistance: Tested according to ISO 26987:2008, no effect from sodium hydroxide solution (25%) or hydrochloric acid solution (3%)

Certifications: ISO9001, ISO14001, ISO45001

CE Certification (European Union)

Industry Awards:

Top 10 Brands in China's Resilient Flooring Industry (2024, 2023, 2022, 2021)

Top 10 Well-Known Brands in China's Resilient Flooring Industry (2018)

Leading Brand in China's Sports Flooring Industry (2017)

Top 10 Circulation Brands in China's Resilient Flooring Industry (2016)